POSSIBLE REASONS OF THE NONPROPORTIONALITY OF RESPONSE

IN NaI:Tl AND CsI:Tl

Kudin, A.M.; Gres’, V.Yu.

The light output is non proportional to electron energy for many scintillation materials at excitation by external gamma-rays. For NaI:Tl and CsI:Tl the non-proportionality manifests itself as increase of a specific light yield L/E with decrease of photon energy E. For NaI:Tl the L/E reaches its maximum value nearly 45 keV on the L/E vs E curve which has two downfalls near L- and K-edge of iodine absorption. In the model of scintillation crystal proposed by Zerby et al [1] a non-proportionality is postulated as an absolute property of material. However, it is well known that the L is proportional to the E for internal sources of radiation [2].

Recently we have revealed the effect of changing of the decay time for photons of different energy [3]. Duration of scintillation is e considerably shorter for X-rays of 5.9 keV energy then for gamma-rays of 662 keV. This effect allows to explain the contradiction noted above. The typical dependence of the L/E vs E for NaI:Tl or CsI:Tl is a sum result of two effects:

- shortening of the scintillation duration, that results in increase of a measured value of the L/E with decrease of photon energy at fixed shaping time;

- influences of a "dead" layer, that is exhibited in quenching of the luminescence near the crystal surface.

In our opinion, non-proportionality of the response reflects the existence of axial non-uniformity of scintillation efficiency. Scintillation efficiency depends on a penetration depth (H) of radiation to the extent of the decay time dependence on the point of interaction. Such approach allows to explain a discrepancy of the L/E near the K-edge of iodine absorption where the H changes almost ten times. A downfall near K-edge always exists on the dependence of the L/E vs E and disappears on the L/E vs H one.

References

1. Zerby C.D., Meyer A. and Murray R.B. Nucl. Inst. Meth. 12 (1961) 115.

2. Leutz H., D'Ambrosio C. IEEE Trans. Nucl. Sci. 44 (1997) 190.

3. Кudin A.M., et al. Functional Materials 9 (2002) 229.

POSSIBLE REASONS OF THE RESPONSE NONPROPORTIONALITY IN NaI-Tl and CsI-Tl

Light output is non proportional to electron energy for many scintillation materials at excitation by external gamma-rays. For NaI-Tl and CsI-Tl the non-proportionality reveals itself as increase of a specific light yield L/E with photon energy E reduction. In the model of scintillation crystal proposed by Zerby et al [1] non-proportionality is postulated as an intrinsic property of material. However it is well known that L is proportional to E for internal sources of radiation [2].

Recently we have revealed the effect decay time reduction for photons of different energy [3]. Duration of scintillation is considerably shorter for X-rays of 5.9 keV energy then for gamma-rays of 662 keV. This effect allows to explain this contradiction. Typical dependence of the L/E vs E for NaI-Tl or CsI-Tl is a sum result of two effects; they are the following:

- shortening of the scintillation duration, that results in an increase of a measured value of the L/E with decrease of photon energy at fixed shaping time;

- influence of a "dead" layer, that is revealed in quenching of the luminescence near the crystal surface.

In our opinion, non-proportionality of the response reflects the existence of axial non-uniformity of scintillation efficiency. Scintillation efficiency depends on a penetration depth (H) of radiation to the extent of the decay time dependence on the point of interaction. This approach allows us to explain discrepancy of the L/E near the K-edge of iodine absorption where the H changes almost by ten times. A downfall near K-edge always exists on the curve of L/E vs E and disappears on the curve L/E vs H.

References

1. Zerby C.D., Meyer A. and Murray R.B. Nucl. Inst. Meth. 12 (1961) 115.

2. Leutz H., D'Ambrosio C. IEEE Trans. Nucl. Sci. 44 (1997) 190.

3. Кudin A.M., et al. Functional Materials 9 (2002) 229.

The light yield (L) is non proportional to energy (E) for many scintillation materials at excitation by external gamma-rays. However it is known that the L is proportional to the E for internal sources of radiation. To eliminate this contradiction we proposed that observed non-proportionality is a sum result of two effects: (i) shortening of the scintillation duration, that results in increase of a measured value of the L/E with decrease of photon energy at fixed shaping time and (ii) influences of a "dead" layer, that is exhibited in quenching of the luminescence near the crystal surface. In our opinion, non-proportionality of the response reflects the existence of axial non-uniformity of scintillation efficiency. Scintillation efficiency depends on a penetration depth (H) of radiation to the extent of the decay time dependence on the point of interaction. Such approach allows to explain a discrepancy of the L/E near the K-edge of iodine absorption where the H changes almost ten times. A downfall near K-edge always exists on the dependence of the L/E vs E and disappears on the L/E vs H one.